Bioelectroventing: an electrochemical-assisted bioremediation strategy for cleaning-up atrazine polluted soils

Ainara Domínguez-Garay a,+, Jose Rodrigo Quejigo a,+, Ulrike Dörfler b, Reiner Schroll b and Abraham Esteve-Núñez ac*

a University of Alcalá. Alcalá de Henares, Madrid, Spain.

b Helmholtz Zentrum München. Múnich, Germany.

c IMDEA-WATER Parque Tecnológico de Alcalá. Madrid, Spain.

+ Ainara Domínguez-Garay and Jose Rodrigo Quejigo are equally contributors

14C-ATR adsorption assays in different electro-conductive materials

Several adsorption assays were conducted to investigate the adsorption of 14C-ATR on different conductive materials: graphite plate, graphite paper, carbon felt and graphite rod. 50 mL eppendorf tubes were filled with 39 mL of deionized water and 14C-ATR standard was added to vide a final concentration of 2.5 μg/μL and a specific radioactivity of 63 Bq·μg-1. Three replicates were conducted for each electrode material and the eppendorf tubes were shaken overhead continuously. At different time intervals aliquots of 1 mL were sampled to measure the radioactivity until the equilibrium for adsorption of 14C-ATR was reached. Each sample was mixed with 4 mL Ultima Gold XR and measured in a liquid scintillation counter (Tricarb 1900 TR, Packard, Dreieich, Germany). A control was performed under the same conditions but in the absence of material.

The higher adsorption was observed in graphite paper, that after 18 hours in incubation 86% of the applied 14C-ATR was retained in the material. The rest of materials showed lower adsorption behaviour than the graphite paper:  7.7% in graphite plate, 2.2% in carbon felt and 1.2% in graphite rod (Figure S1).  Regarding to the results and considering the convenience physico-mechanical properties, the high surface area, and the inexpensive cost, the material used to conform the electrodes for mineralization assays was carbon felt and graphite rod.

A

B

C

D

Figure S1. 14C-ATR adsorption in different electrode conductive material: graphite paper (A), graphite plate (B), carbon felt (C) and graphite rod (D)