SUPPLEMENTARY INFORMATION

Acidic Wood Extractives Accelerate the Curing Process of Emulsion Polymer Isocyanate (EPI) Adhesives

Merve Özparpucu1,*, Antoni Sánchez-Ferrer1,*, Mathias Schuh1, Bianca Wilhelm1, Riddhiman Sarkar2,3, Bernd Reif2,3, Elisabeth Windeisen-Holzhauser1, Klaus Richter1

1 Technical University of Munich, School of Life Sciences Weihenstephan, Chair of Wood Science, Winzererstr. 45, 80797 Munich, Germany.

2 Helmholtz-Zentrum München (HMGU), Deutsches Forschungszentrum für Gesundheit und Umwelt, Ingolstädter Landstr. 1, 85764 Neuherberg, Germany

3 Technical University of Munich, Bayerisches NMR Zentrum (BNMRZ), Department of Chemistry, Lichtenbergstr. 4, 85748 Garching, Germany

* Corresponding authors: e-mail: oezparpucu@hfm.tum.de and sanchez@hfm.tum.de

Supplementary Tables

Table SI-1 Spectral changes related to EPI-curing

| FTIR band (cm-1) | Assignment | The relative changes |  |  |
| --- | --- | --- | --- | --- |
|  |  | EPI-Ref | EPI-Ch | EPI-Oa |
| 3100-3500 | N-H str. Due to the formation of the amine (N-H), urea (NHCON-H), and urethane (OCON-H) moieties, but partly overlaps with OH str. | +28% | +48% | -12% |
| 2270 | NCO str. Isocyanate stretching from the hardener | -31% | -47% | -37% |
| 1730 | CO str. free urethane moiety together with the acetyl moiety | -21% | -5% | -15% |
| 1645 | CO str. carbonyl stretching of H-bonded urea motifs (NHCONH) and partly overlapped with scissoring band of water | +44% | +70% | -2% |

Table SI-2. pKa values for the compounds used in the mixtures with EPI-adhesive.

| Acidic Compounds |  | pKa* |
| --- | --- | --- |
| Gallic acid |  | 3.94 |
| Benzoic acid |  | 4.08 |
| Malonic acid |  | 2.43 |
| Maleic acid |  | 1.83 |
| Succinic acid |  | 3.55 |
| Ellagic acid |  | 5.54 |
| Caffeic acid |  | 3.14 |
| m-Coumaric acid |  | 4 |
| Phenolic compounds |  |  |
| Phloroglucinol |  | 9.13 |
| Hydroquinone |  | 9.68 |
| Sugar alcohol |  |  |
| Xylitol |  | 12.76 |

* Based on the values in ChemAxon.

Table SI-3. Storage shear modulus (G’), segmental molecular weight (Mc) and crosslinking density (c) for the samples EPI-Ref, EPI-Ch and EPI-Oa after 36 h of curing.

| Sample | G' (MPa) | Mc (g/mol) | vc (mol/m3)* |
| --- | --- | --- | --- |
| EPI-Ref | 6.26 | 466 | 2568 |
| EPI-Ch | 7.23 | 403 | 2966 |
| EPI-Oa | 5.61 | 520 | 2302 |

*The density for the cured EPI-adhesive was estimated to be 1.20 g/cm3 at 20 C.

Supplementary Figures

FIGURE SI-1 FTIR spectra comparison: water-based EPI-adhesive components: chestnut extract (green), EPI-emulsion part (grey), EPI-isocyanate based hardener (red), EPI-adhesive (emulsion+hardener at the beginning of rheology measurements, t=0 min) (black), cured EPI-adhesive after ashing at 525 °C for 90 min (blue), and precipitated CaCO3 (orange, NIST database).

a)

b)

FIGURE SI-2 a) The water extraction set-up at room temperature. b) The extracted content after 50 and 80 h of extraction on the chestnut wood panels from which the tensile shear test specimens were prepared.

FIGURE SI-3 Liquid 13C NMR spectra of the polymer EPI-emulsion component (PVA-PVAC, black), the EPI-hardener (pMDI, blue), and the chestnut extract (gallic acid and sugar molecules, red).

FIGURE SI-4 Strain-sweep tests at 1 Hz frequency and 20 °C on the EPI-Ref sample a) at lower strain % values (for the determination of the LVR Region), and b) at higher strain % values (indicating a shear thinning behavior).

FIGURE SI-5 Example of technical variabilities in G‘ curves within the sample groups.

FIGURE SI-6 Derivative curves, dG‘/dt, as a function of time for the samples EPI-Ref (black), EPI-Ch (red) and EPI-Oa (blue) showing the different reaction kinetics for 3 h of measurement.

FIGURE SI-7 PCA scores from the FTIR spectra for the a) EPI-Ref, b) EPI-Ch and EPI-Oa samples

FIGURE SI-8 Loading PC1 comparison for the EPI-Ref, EPI-Ch and EPI-Oa

FIGURE SI-9 PCA Results from the FTIR spectra: a) PC scores of EPI-Ch with 0.17 % extract addition, b) the comparison of the loadings PC1 between the samples.

FIGURE SI-10 Storage shear modulus G’ as a function of time and for different amounts of gallic acid.

FIGURE SI-11 Storage shear modulus G’ as a function of time for some EPI-mixtures with different organic compounds.

FIGURE SI-12  Single Shot Analysis (SSA)-pyrolysis products of the EPI-Ref, EPI-Ch samples and the hardener (at 255 °C).

| a) | b) |
| --- | --- |
| c) |  |

FIGURE SI-13   Storage shear modulus, G’, loss shear modulus, G”, and loss factor, tan  evolution for 6 h for the samples a) EPI-Ref, b) EPI-Ch and c) Derivative curves, dG‘/dt, as a function of time for 6 h of measurement.

| a) | b) |
| --- | --- |
| c) | d) |

FIGURE SI-14   Storage shear modulus, G’, loss shear modulus, G”, and loss factor, tan  evolution for 35 h for the samples a) EPI-Ref, b) EPI-Ch and c) EPI-Oa, and d) Derivative curves, dG‘/dt, as a function of time for 35 h of measurement.

.

FIGURE SI-15   Solid-state 13C NMR of the EPI-Ref sample (black), and the simulated peaks of the urethane (red), urea (green) and free amine (orange) formed during the curing process, and the PVA-PVAc polymer in the EPI-emulsion (blue).

FIGURE SI-16    Solid-state 13C NMR of the chestnut extract (black), and the simulated peaks of gallic acid (red), inositol (green), and sugars (C6 and C5, blue).

FIGURE SI-17   Solid-state 13C NMR spectra for the a) EPI-Ch (0.93%) and b) EPI-Oa (0.17%). The fitting curves (red) and the corresponding extract (blue) are evaluated from the deconvolution process. The results indicate 0.98% and 0.35% of extractives for the EPI-Ch and EPI-Oa samples, respectively.