Supplementary information

Table S1: Morphological data for different shaped particles calculated via the BioVoxxel plugin in the ImageJ software

| particle shape |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| aspect ratio | 1.00 | 0.70 | 0.91 | 0.50 | 0.50 |
| extent bulkiness | 0.79 | 0.71 | 0.69 | 0.80 | 0.74 |
| compactness | 1.00 | 0.8 | 0.90 | 0.71 | 0.69 |
| circularity | 1.00 | 0.89 | 0.89 | 0.88 | 0.73 |
| roundness | 1.00 | 0.64 | 0.80 | 0.51 | 0.47 |
| solidity | 1.00 | 1.00 | 1.00 | 1.00 | 0.86 |
| convexity | 1.00 | 1.00 | 1.00 | 1.00 | 0.90 |
| ellipticity | 1.00 | 1.00 | 1.05 | 2.00 | 1.91 |
| elongation | 0.00 | 0.00 | 0.07 | 1.00 | 0.93 |

Table S2: Number of particles found per sample measured via AZtec Features (Oxford)

|  | Particles found per sample |  |  |
| --- | --- | --- | --- |
| Date | W15 | F15 | F5 |
| 17/5/2022 | 21622 | 31895 | 5426 |
| 19/7/2022 | 7765 | 31400 | 10194 |
| 28/8/2022 | 17789 | 61544 | 11121 |

Figure S1: Energy-by-position distribution of a 5 kV electron beam in a Fe2O3 substrate, simulated via the trajectories of 2500 electrons in the Monte Carlo Software.

Figure S2: X-ray intensity of Fe and O as a function of the penetration depth of a 5 kV electron beam in a Fe2O3 substrate, simulated via the trajectories of 2500 electrons in the Monte Carlo Software.

Figure S3: Average classification values for W15 samples

Figure S4: Average classification results of particles smaller than 1 µm for filter samples measured at 5 kV

Table S3: Classification scheme for particles on PC filters measured at 5 kV and 15 kV

| Class | Subclass | Criteria | Min | Max | Special rule |
| --- | --- | --- | --- | --- | --- |
| Oversized (F5 only) |  | DA (µm) | 1 | 100 | Reject if matched (F5 samples only) |
| Non-ferrous metals | Class rule | Oxygen | 20 | 100 | Exclude if matched |
|  | Cu | Copper | 5 | 100 | Must be detected |
|  | W | Tungsten | 2 | 100 | Must be detected |
|  | Ti | Titanium | 5 | 100 | Must be detected |
|  | Sn | Tin | 5 | 100 | Must be detected |
|  |  | Copper | 5 | 100 | Exclude if matched |
|  | Pb | Lead | 5 | 100 | Must be detected |
|  |  | Copper | 5 | 100 | Exclude if matched |
|  | Cd | Cadmium | 1 | 100 | Must be detected |
| Brake wear | Class rule | Sulphur | 1 | 100 | Must be detected |
|  | SbS3 | Antimony | 1 | 100 | Must be detected |
|  | BaSO4 | Barium | 1 | 100 | Must be detected |
| Ferrous metals | Class rule | Oxygen | 20 | 100 | Exclude if matched |
|  |  | Iron | 5 | 100 | Must be detected |
|  | Steel - Low alloy | Nickel | 2 | 100 | Exclude if matched |
|  |  | Manganese | 0 | 4 |  |
|  |  | Chromium | 0 | 1.5 |  |
|  | Steel - Cr | Manganese | 1 | 100 | Exclude if matched |
|  |  | Chromium | 1 | 20 | Must be detected |
|  |  | Nickel | 2 | 100 | Exclude if matched |
|  | Steel - High alloy | Nickel | 2 | 100 | Must be detected |
|  |  | Chromium | 2 | 100 | Must be detected |
| Al Alloys | Class rule | Aluminium | 75 | 100 | Must be detected |
|  |  | Oxygen | 10 | 100 | Exclude if matched |
|  |  | Manganese | 0 | 5 |  |
|  | Al | Magnesium | 0 | 0.5 |  |
|  |  | Aluminium | 75 | 100 | Must be detected |
|  |  | Silicon | 0 | 0.5 |  |
|  | Al (Mg) | Magnesium | 0.5 | 5 | Must be detected |
|  |  | Silicon | 0 | 1 |  |
|  | Al (Mg,Si) | Magnesium | 0.5 | 10 | Must be detected |
|  |  | Silicon | 0.5 | 10 | Must be detected |
| Non-ferrous oxides | Class rule | Oxygen | 20 | 100 | Must be detected |
|  |  | Iron | 30 | 100 | Exclude if matched |
|  | Ba-oxide | Barium | 1 | 100 | Must be detected |
|  |  | Titanium | 1 | 100 | Exclude if matched |
|  |  | Sulfur | 1 | 100 | Exclude if matched |
|  | Ti-oxide | Titanium | 5 | 75 | Must be detected |
|  | Zr-oxide | Zirconium | 10 | 75 | Must be detected |
|  |  | Silicon | 5 | 100 | Exclude if matched |
|  | Zn-oxide | Zinc | 15 | 50 | Must be detected |
|  | Cu-oxide | Cu | 5 | 100 | Must be detected |

Table S3: Classification scheme for particles on PC filters measured at 5 kV and 15 kV (continued)

| Class | Subclass | Criteria | Min | Max | Special rule |
| --- | --- | --- | --- | --- | --- |
| Iron oxide |  | Iron | 18 | 100 | Must be detected |
|  |  | Oxygen | 20 | 100 | Must be detected |
| Al-Si-Oxides | Class rule | Oxygen | 20 | 100 | Must be detected |
|  | Al-Oxide | Aluminium | 15 | 100 | Must be detected |
|  |  | Silicon | 5 | 100 | Exclude if matched |
|  |  | Iron | 5 | 100 | Exclude if matched |
|  |  | Copper | 5 | 100 | Exclude if matched |
|  |  | Tungsten | 2 | 100 | Exclude if matched |
|  | Si-Oxide | Silicon | 15 | 100 | Must be detected |
|  |  | Aluminium | 1 | 50 | Exclude if matched |
|  |  | Iron | 20 | 100 | Exclude if matched |
|  | Silicates | Aluminium | 5 | 100 | Must be detected |
|  |  | Silicon | 5 | 100 | Must be detected |
|  |  | Copper | 5 | 100 | Exclude if matched |
|  |  | Tungsten | 2 | 100 | Exclude if matched |
|  | Zircon | Zirconium | 5 | 100 | Must be detected |
|  |  | Silicon | 5 | 100 | Must be detected |
|  |  | Iron | 30 | 100 | Exclude if matched |
| Salts & carbonates | Class rule | Silicon | 10 | 100 | Exclude if matched |
|  | Salt | Chlorine | 5 | 100 | Must be detected |
|  |  | Aluminium | 5 | 100 | Exclude if matched |
|  |  | Copper | 5 | 100 | Exclude if matched |
|  |  | Zinc | 5 | 100 | Exclude if matched |
|  |  | Cadmium | 1 | 100 | Exclude if matched |
|  |  | Iron | 5 | 100 | Exclude if matched |
|  | CaSO4 | Calcium | 5 | 100 | Must be detected |
|  |  | Sulfur | 5 | 100 | Must be detected |
|  |  | Oxygen | 20 | 100 | Must be detected |
|  |  | Silicon | 5 | 100 | Exclude if matched |
|  |  | Chlorine | 10 | 100 | Exclude if matched |
|  | CaCO3 & CaO | Oxygen | 20 | 100 | Must be detected |
|  |  | Sodium | 0 | 15 |  |
|  |  | Sulfur | 0 | 2 |  |
|  |  | Calcium | 10 | 60 | Must be detected |
|  |  | Silicon | 10 | 100 | Exclude if matched |
|  | Al-chloride | Silicon | 10 | 100 | Exclude if matched |
|  |  | Chlorine | 10 | 100 | Must be detected |
|  |  | Aluminium | 10 | 100 | Must be detected |
|  | Nitrates | Oxygen | 60 | 100 | Must be detected |
|  |  | Nitrogen | 15 | 50 | Must be detected |
| Critical fibers |  | Aspect ratio | 3 | 250 | Must be detected |
|  |  | Lenght (µm) | 5 | 100 | Must be detected |
| Carbonaceous |  | Oxygen | 75 | 100 | Must be detected |

Table S4: Classification scheme for particles found on Si wafers measured at 15 kV

| Class | Subclass | Criteria | Min | Max | Special rule |
| --- | --- | --- | --- | --- | --- |
| Wafer |  | Oxygen | 95 | 100 | reject if matched |
| Ag-paint |  | Silver | 10 | 100 | reject if matched |
| Non-ferrous metals | Class rule | Oxygen | 20 | 100 | Exclude if matched |
|  | Cu | Copper | 5 | 100 | Must be detected |
|  | W | Tungsten | 2 | 100 | Must be detected |
|  | Ti | Titanium | 5 | 100 | Must be detected |
|  | Sn | Tin | 5 | 100 | Must be detected |
|  |  | Copper | 5 | 100 | Exclude if matched |
|  | Pb | Lead | 5 | 100 | Must be detected |
|  |  | Copper | 5 | 100 | Exclude if matched |
|  | Cd | Cadmium | 1 | 100 | Must be detected |
| Brake wear | Class rule | Sulfur | 1 | 100 | Must be detected |
|  | SbS3 | Antimony | 1 | 100 | Must be detected |
|  | BaSO4 | Barium | 1 | 100 | Must be detected |
| Ferrous metals | Class rule | Oxygen | 20 | 100 | Exclude if matched |
|  |  | Iron | 5 | 100 | Must be detected |
|  | Steel - Low alloy | Nickel | 2 | 100 | Exclude if matched |
|  |  | Manganese | 0 | 4 |  |
|  |  | Chromium | 0 | 1.5 |  |
|  | Steel - Cr | Manganese | 1 | 100 | Exclude if matched |
|  |  | Chromium | 1 | 20 | Must be detected |
|  |  | Nickel | 2 | 100 | Exclude if matched |
|  | Steel - High alloy | Nickel | 2 | 100 | Must be detected |
|  |  | Chromium | 2 | 100 | Must be detected |
| Al Alloys | Class rule | Aluminium | 75 | 100 | Must be detected |
|  |  | Oxygen | 10 | 100 | Exclude if matched |
|  |  | Manganese | 0 | 5 |  |
|  | Al | Magnesium | 0 | 0.5 |  |
|  | Al (Mg) | Magnesium | 0.5 | 5 | Must be detected |
| Non-ferrous oxides | Class rule | Oxygen | 20 | 100 | Must be detected |
|  |  | Iron | 30 | 100 | Exclude if matched |
|  | Ba-oxide | Barium | 1 | 100 | Must be detected |
|  |  | Titanium | 1 | 100 | Exclude if matched |
|  |  | Sulfur | 1 | 100 | Exclude if matched |
|  | Ti-oxide | Titanium | 5 | 75 | Must be detected |
|  | Zr-oxide | Zirconium | 10 | 75 | Must be detected |
|  | Zn-oxide | Zinc | 15 | 50 | Must be detected |
|  | Cu-oxide | Cu | 5 | 100 | Must be detected |
| Iron oxide |  | Iron | 18 | 100 | Must be detected |
|  |  | Oxygen | 20 | 100 | Must be detected |

Table S4: Classification scheme for particles found on Si wafers measured at 15 kV (continued)

| Al-Oxides |  | Oxygen | 20 | 100 | Must be detected |
| --- | --- | --- | --- | --- | --- |
|  |  | Aluminium | 15 | 100 | Must be detected |
|  |  | Iron | 5 | 100 | Exclude if matched |
|  |  | Copper | 5 | 100 | Exclude if matched |
| Class | Subclass | Criteria | Min | Max | Special rule |
| Salts & carbonates | Salt | Chlorine | 5 | 100 | Must be detected |
|  |  | Aluminium | 5 | 100 | Exclude if matched |
|  |  | Copper | 5 | 100 | Exclude if matched |
|  |  | Zinc | 5 | 100 | Exclude if matched |
|  |  | Cadmium | 1 | 100 | Exclude if matched |
|  |  | Iron | 5 | 100 | Exclude if matched |
|  | CaSO4 | Calcium | 5 | 100 | Must be detected |
|  |  | Sulfur | 5 | 100 | Must be detected |
|  |  | Oxygen | 20 | 100 | Must be detected |
|  |  | Chlorine | 10 | 100 | Exclude if matched |
|  | CaCO3 & CaO | Oxygen | 20 | 100 | Must be detected |
|  |  | Sodium | 0 | 15 |  |
|  |  | Sulfur | 0 | 2 |  |
|  |  | Calcium | 10 | 60 | Must be detected |
|  | Al-chloride | Chlorine | 10 | 100 | Must be detected |
|  |  | Aluminium | 10 | 100 | Must be detected |
|  | Nitrates | Oxygen | 60 | 100 | Must be detected |
|  |  | Nitrogen | 15 | 50 | Must be detected |
| Critical fibers |  | Aspect ratio | 3 | 250 | Must be detected |
|  |  | Length (µm) | 5 | 100 | Must be detected |
| Carbonaceous | Organic carbon | Oxygen | 10 | 60 | Must be detected |
|  |  | Carbon | 40 | 90 | Must be detected |
|  |  | Oxygen + Carbon | 90 | 100 | Must be detected |
|  | Elemental carbon | Oxygen | 99 | 100 | Must be detected |

Table S5: Elemental composition of Cu rich particles found in the Munich subway

| Concentration in wt. % | Filter 15 kV |  |  | Wafer 15 kV |  |  | Filter 5 kV |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cu | 30.38 | ± | 28.02 | 36.83 | ± | 23.36 | 22.12 | ± | 17.84 |
| O | 29.05 | ± | 9.87 | 12.78 | ± | 9.25 | 51.78 | ± | 16.39 |
| Fe | 37.90 | ± | 23.79 | 14.92 | ± | 19.93 | 10.86 | ± | 13.23 |
| C | ND |  |  | 29.15 | ± | 13.3 | ND |  |  |
| Si | 1.12 | ± | 1.99 | ND |  |  | 14.39 | ± | 8.15 |
| other Elements | 2.68 | ± | 6.50 | 6.32 | ± | 16.34 | 0.85 | ± | 3.29 |