Supplementary file:

Neddylation suppression by a macrophage membrane-coated nanoparticle promotes dual immunomodulatory repair of diabetic wounds

Figure S1. (A) Western blot was used to detect the protein expression of NEDD8-Cullins, Cyclin D1, VEGF-A and ACTB in the skin tissue of normal and diabetic mice.

(B, C) The FACS histogram depicted the flow cytometry findings of RAW264.7 macrophages that were cultured for 24 hours with LPS and then with various treatments for 24 hours.

Figure S2. (A, D) The proliferation of L929 mouse fibroblast cell lines was observed by calcein-AM staining on days 1 and 3. Scale bar: 100 μm.

(B, C) The wound healing rate of each group was quantitatively evaluated by L929 mouse fibroblast cell lines in vitro. Scale bar: 100 μm.

Figure S3. (A) Swelling ratio of the porous Gelma hydrogel in PBS at 37 °C

(B) Degradation ratio of the porous Gelma hydrogel.

(C) TEM image of GelMA hydrogel without nanoparticles. Scale bar: 100 μm.

(D) TEM image of GelMA hydrogel without nanoparticles loaded with M-NPs. Scale bar: 100 μm.

Figure S4. (A) After 1 day culture of HUVECs with different treatments, the cell biocompatibility was assessed using the CCK-8 method.

(B, C) Representative images and wound healing closure rates of full-thickness defects in diabetic rats at days 0, 3, 7, 10, and 14 after receiving treatment with PBS (Con), GelMA, GelMA@NPs without MLN4924, GelMA@NPs/MLN4924, and GelMA@M-NPs/MLN4924.

Here, we added the MLN4924 group in cell and animal experiments to evaluate its effects on cells and diabetic mice. Firstly, we conducted CCK8 tests on HUVECs in normal culture conditions and found no statistically significant differences in cell viability among the different groups (Figure S4A). Subsequently, we further investigated this influence in diabetic mice. As shown in Figure S4B and S4C, the MLN4924 group exhibited wound healing trends similar to those of the high glucose group and the GelMA group, with overall trends consistent with previous animal experiments. Additionally, Figure S6 demonstrated excellent biocompatibility among all treatment groups, including the GelMA@NPs without MLN4924 group. In summary, MLN4924 did not exhibit noticeable toxicity or inhibitory effects on wound healing in diabetic mice, nor did it demonstrate significant promotive effects.

Figure S5. Western blot was used to detect the protein expression of NEDD8-Cullins, VEGF-A and ACTB in the skin tissue of normal and different treatment group of diabetic mice.

Figure S6. The H&E staining of the major organs from the healthy mice with different treatments. Scale bar: 100 μm.