An efficient screening of dissolution modulators of Mg alloys: Combining high-throughput multi-well exposure with topographical quantification of volume loss and pitting corrosion

Ci Song a, *, Bahram Vaghefinazari a, Tim Würger a, Anna Lisitsyna b, Di Mei c, Maria Nienaber d, Jan Bohlen d, Mikhail L. Zheludkevich a, e, f, Shadi Albarqouni b, g, Christian Feiler a, f, Sviatlana V. Lamaka a*.

a Institute of Surface Science, Helmholtz-Zentrum Hereon, Geesthacht 21502, Germany

b Helmholtz AI, Helmholtz Center Munich, Neuherberg 85764, Germany

c School of Materials Science and Engineering & Henan Key Laboratory of Advanced Magnesium Alloy, Zhengzhou University, Zhengzhou 450001, PR China

d Institute of Material and Process Design, Helmholtz-Zentrum Hereon, Geesthacht 21502, Germany

e Institute for Materials Science, Faculty of Engineering, Kiel University, Kiel 24103, Germany

f Kiel Nano, Surface and Interface Science KiNSIS, Kiel University, Kiel 24103, Germany

g University Hospital Bonn, University of Bonn, Bonn 53127, Germany

*Corresponding authors: Ci.Song@hereon.de (Ci Song) and Sviatlana.Lamaka@hereon.de (Sviatlana Lamaka)

Figure S1 Schematic representation of the bath for acid etching pre-treatment and chromic acid cleaning, used for removing the corrosion products.

Table S1 The elemental composition of the extruded AZ31 alloy. The values are in ppm or in wt.% when indicated.

| Element | Al | Cu | Mn | Fe | Ni | Zn | Si | Ca | Sn | Zr | Ce | La | Mg |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Weight Composition | 2.70±0.02% | 27 | 0.22% | 20±1 | 2±0.5 | 0.87±0.01% | 158±2.0 | <1 | <5 | <3 | 1 | <1 | 94.19% |

|  | Before chromic acid cleaning | After chromic acid cleaning |
| --- | --- | --- |
| 1-1 |  |  |
| 1-2 |  |  |
| 1-3 |  |  |
| 1-4 |  |  |
| 1-5 |  |  |
| 1-6 |  |  |
| 2-1 |  |  |
| 2-2 |  |  |
| 2-3 |  |  |
| 2-4 |  |  |
| 2-5 |  |  |
| 3-1 |  |  |
| 3-2 |  |  |
| 3-3 |  |  |
| 3-4 |  |  |
| 3-5 |  |  |
| 3-6 |  |  |
| 4-1 |  |  |
| 4-2 |  |  |
| 4-3 |  |  |
| 4-4 |  |  |
| 4-5 |  |  |
| 4-6 |  |  |
| 5-1 |  |  |
| 5-2 |  |  |
| 5-3 |  |  |
| 5-4 |  |  |
| 5-5 |  |  |
| 5-6 |  |  |

Figure S2 Optical images of the first five groups of samples before and after chromic acid cleaning as captured by the table-top scanner.

Table S2 Commercial names of tested dissolution modulators, and their corresponding CAS number, concentration, inhibition efficiency, inhibition power, symmetrized inhibition efficiency calculated by profilometric weight loss and pitting factor ((IE-P, IEsym-P, and IP-P,), PF). (Red: accelerator, IE < -40%; green: inhibitor, IE > 50%). The initial pH of all solutions was adjusted to 7.0 ± 0.5. The room temperature of the airconditioned lab during the immersion was 22 ± 2 ℃ and the humidity was 75 ± 5%. The average value and standard deviation are based on four replicates measurements for most results and three parallel measurements for few results.

| Concentration (mM) | Dissolution modulator | Structure | CAS number | IE-P (%) | IEsym-P (%) | IP-P | PF |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Dissolution modulators for validation |  |  |  |  |  |  |  |
| 50 | Benzotriazole |  | 95-14-7 | -107 ± 16 | -52 ± 4 | -3.17 ± 0.35 | 30.0 ± 7.0 |
| 50 | 3,5-Dimethylpyrazole |  | 67-51-6 | -24 ± 30 | -19 ± 20 | -0.93 ± 1.05 | 19.1 ± 5.9 |
| 50 | 1,2,4-Triazole |  | 288-88-0 | -283 ± 21 | -74 ± 1 | -5.83 ± 0.21 | 17.9 ± 5.4 |
| 50 | Hexamethyleneteramine |  | 100-97-0 | -52 ± 35 | -34 ± 14 | -1.82 ± 0.94 | 20.3 ± 4.8 |
| 50 | 5,5-Dimethylhydantoin |  | 77-71-4 | -312 ± 22 | -76 ± 1 | -6.15 ± 0.22 | 18.7 ± 1.2 |
| 50 | Piperazine |  | 110-85-0 | -34 ± 10 | -25 ± 5 | -1.27 ± 0.31 | 17.4 ± 3.5 |
| 50 | 4-Isopropylbenzoic acid |  | 536-66-3 | 14 ± 7 | 14 ± 7 | 0.64 ± 0.37 | 21.7 ± 7.5 |
| 50 | 4-Tert-butylbenzoic acid |  | 98-73-7 | 0 ± 19 | 0 ± 19 | 0 ± 0.87 | 25.0 ± 7.3 |
| 50 | 3-Methyl-2-nitrobenzoic acid |  | 5437-38-7 | -248 ± 25 | -71 ± 2 | -5.42 ± 0.31 | 6.8 ± 1.7 |
| saturated | 2'-Hydroxy-4'-methoxyaceto-phenone |  | 552-41-0 | 23 ± 19 | 23 ± 19 | 1.16 ± 1.19 | 21.6 ± 3.1 |
| 50 | Mandelic acid |  | 90-64-2 | 11 ± 19 | 11 ± 19 | 0.49 ± 0.95 | 25.7 ± 5.8 |
| saturated | 1-Pheny-1,3-butanedione |  | 93-91-4 | -6 ± 22 | -6 ± 21 | -0.26 ± 1.01 | 26.6 ± 9.2 |
| saturated | Maltol |  | 118-71-8 | -155 ± 4 | -61 ± 1 | -4.06 ± 0.07 | 20.4 ± 15.6 |
| 50 | Glycolic acid |  | 79-14-1 | 33 ± 10 | 33 ± 10 | 1.71 ± 0.64 | 31.2 ± 3.4 |
| 50 | Oxalic acid |  | 144-62-7 | 32 ± 16 | 32 ± 16 | 1.67 ± 0.98 | 20.1 ± 3.4 |
| 50 | Lactic acid |  | 50-21-5 | -57 ± 17 | -36 ± 7 | -1.97 ± 0.48 | 23.0 ± 7.3 |
| 50 | Maleic acid |  | 203-742-5 | -1 ± 35 | -1 ± 30 | -0.02 ± 0.58 | 14.9 ± 3.0 |
| 50 | Malonic acid |  | 141-82-2 | 5 ± 24 | 5 ± 23 | 0.24 ± 1.19 | 18.8 ± 4.7 |
| 50 | Succinic acid |  | 110-15-6 | -7 ± 34 | -6 ± 27 | -0.28 ± 1.43 | 22.7 ± 6.8 |
| 50 | Alginic acid sodium salt from brown algae |  | 9005-32-7 | 41 ± 6 | 41 ± 6 | 2.27 ± 0.46 | 43.3 ± 6.0 |
| Saturated | Chitosan |  | 9012-76-4 | 18 ± 2 | 18 ± 2 | 0.88 ± 0.11 | 23.6 ± 6.3 |
| 50 | Dextran |  | 9004-54-0 | 26 ± 12 | 26 ± 12 | 1.32 ± 0.75 | 25.4 ± 1.7 |
| 50 | Penicillin G Na salt |  | 69-57-8 | -39 ± 25 | -28 ± 13 | -1.44 ± 0.78 | 40.4 ± 2.4 |
| 50 | Folic acid |  | 59-30-3 | -3 ± 20 | -3 ± 18 | -0.14 ± 0.86 | 23.0 ± 7.3 |
| All dissolution modulators |  |  |  |  |  |  |  |
| 3.5 wt. % | Sodium chloride (NaCl) |  | 7647-14-5 |  |  |  | 19.7 ± 5.2 |
| 50 | Glycolic acid |  | 79-14-1 | 33 ± 10 | 33 ± 10 | 1.71 ± 0.64 | 31.2 ± 3.4 |
| 50 | Oxalic acid |  | 144-62-7 | 32 ± 16 | 32 ± 16 | 1.67 ± 0.98 | 20.1 ± 3.4 |
| 50 | Lactic acid |  | 50-21-5 | -57 ± 17 | -36 ± 7 | -1.97 ± 0.48 | 23.0 ± 7.3 |
| 50 | Maleic acid |  | 203-742-5 | -1 ± 35 | -1 ± 30 | -0.02 ± 1.58 | 14.9 ± 3.0 |
| 50 | Malonic acid |  | 141-82-2 | 5 ± 24 | 5 ± 23 | 0.24 ± 1.19 | 18.8 ± 4.7 |
| 50 | Itaconic acid |  | 97-65-4 | 12 ± 14 | 12 ± 14 | 0.54 ± 0.70 | 17.4 ± 3.6 |
| 50 | Succinic acid |  | 110-15-6 | -7 ± 34 | -6 ± 27 | -0.28 ± 1.43 | 22.7 ± 6.8 |
| 50 | Sodium formate |  | 141-53-7 | 32 ± 6 | 32 ± 6 | 1.7 ± 0.42 | 21.8 ± 1.1 |
| 50 | Dimethylolpropionic acid |  | 4767-03-7 | 37 ± 8 | 37 ± 8 | 2.03 ± 0.59 | 23.3 ± 4.4 |
| 50 | Diglycolic acid |  | 110-99-6 | 22 ± 8 | 22 ± 8 | 1.1 ± 0.41 | 21.6 ± 8.0 |
| 50 | Citraconic acid |  | 498-23-7 | 29 ± 10 | 29 ± 10 | 1.51 ± 0.60 | 17.1 ± 4.5 |
| 50 | Acetic acid |  | 64-19-7 | 21 ± 14 | 21 ± 14 | 1 ± 0.78 | 21.2 ± 4.1 |
| 50 | Citric acid |  | 77-92-9 | -279 ± 32 | -74 ± 5 | -5.79 ± 0.35 | 20.4 ± 1.5 |
| 50 | Tartaric acid, (L-(+)-Tartaric acid |  | 87-69-4 | 48 ± 17 | 48 ± 17 | 2.86 ± 1.60 | 33.3 ± 7.2 |
| saturated | Stearic acid sodium salt |  | 822-16-2 | -37 ± 11 | -27 ± 6 | -1.36 ± 0.35 | 8.8 ± 0.9 |
| 50 | Fumaric acid |  | 110-17-8 | 58 ± 7 | 58 ± 7 | 3.75 ± 0.71 | 41.7 ± 17.4 |
| 50 | Malic acid |  | 6915-15-7 | 39 ± 27 | 39 ± 27 | 2.13 ± 2.63 | 26.3 ± 7.2 |
| 50 | Potassium oxalate monohydrate |  | 6487-48-5 | 47 ± 9 | 47 ± 9 | 2.78 ± 0.76 | 24.4 ± 8.3 |
| 50 | Potassium L-tartrate monobasic |  | 868-14-4 | 32 ± 15 | 32 ± 15 | 1.66 ± 0.86 | 27.0 ± 7.6 |
| 50 | Sodium citrate tribasic dihydrate |  | 6132-04-3 | 47 ± 7 | 47 ± 7 | 2.72 ± 0.52 | 20.3 ± 11.2 |
| 50 | 1,2,3,4-Butanetetracarboxylic acid |  | 1703-58-8 | 33 ± 9 | 33 ± 9 | 1.71 ± 0.61 | 28.8 ± 5.5 |
| 50 | Tricarballylic acid |  | 99-14-9 | -19 ± 7 | -16 ± 5 | -0.75 ± 0.26 | 21.0 ± 7.3 |
| 50 | Tartronic acid |  | 80-69-3 | 15 ± 13 | 15 ± 13 | 0.73 ± 0.66 | 16.0 ± 3.2 |
| 50 | Adipic acid |  | 124-04-9 | -13 ± 22 | -12 ± 15 | -0.55 ± 0.79 | 22.4 ± 3.6 |
| 50 | Ascorbic acid |  | 50-81-7 | -29 ± 11 | -22 ± 6 | -1.1 ± 0.37 | 19.9 ± 2.8 |
| 50 | Cyclohexaneacetic acid |  | 5292-21-7 | 1 ± 7 | 1 ± 7 | 0.05 ± 0.33 | 21.9 ± 4.1 |
| 50 | Quinic acid |  | 77-95-2 | 26 ± 9 | 26 ± 9 | 1.29 ± 0.51 | 18.5 ± 3.0 |
| 50 | Cyclohexanemethanol |  | 100-49-2 | 15 ± 21 | 15 ± 21 | 0.7 ± 1.12 | 21.0 ± 2.2 |
| 50 | D-Pinitol |  | 10284-63-6 | -10 ± 10 | -9 ± 8 | -0.41 ± 0.38 | 20.1 ± 3.5 |
| 50 | Tetrahydrofuran |  | 109-99-9 | -46 ± 32 | -32 ± 17 | -1.65 ± 0.99 | 22.3 ± 4.8 |
| 50 | D-(+)-Galactose |  | 59-23-4 | 4 ± 21 | 4 ± 21 | 0.16 ± 1.06 | 21.2 ± 6.1 |
| 50 | Glucose |  | 50-99-7 | 3 ± 19 | 3 ± 19 | 0.13 ± 0.85 | 24.6 ± 2.8 |
| 50 | β-Lactose |  | 5965-66-2 | -15 ± 6 | -13 ± 5 | -0.63 ± 0.24 | 17.4 ± 0.7 |
| 50 | Lactobionic acid |  | 96-82-2 | 40 ± 3 | 40 ± 3 | 2.21 ± 0.24 | 29.2 ± 3.1 |
| 50 | Alginic acid sodium salt from brown algae |  | 9005-32-7 | 41 ± 6 | 41 ± 6 | 2.27 ± 0.46 | 43.3 ± 6.0 |
| 50 | Dextran |  | 9004-54-0 | 26 ± 12 | 26 ± 12 | 1.32 ± 0.75 | 25.4 ± 1.7 |
| 50 | Benzoic acid |  | 65-85-0 | 23 ± 6 | 23 ± 6 | 1.16 ± 0.34 | 19.7 ± 4.0 |
| 50 | Phthalic acid |  | 88-99-3 | 9 ± 13 | 9 ± 13 | 0.42 ± 0.64 | 19.0 ± 4.5 |
| 50 | Terephthalic acid |  | 100-21-0 | 46 ± 21 | 46 ± 21 | 2.67 ± 2.00 | 20.1 ± 3.4 |
| 50 | 1,2,3-Benzenetricarboxylic acid hydrate |  | 732304-21-1 | 32 ± 18 | 32 ± 18 | 2.66 ± 0.32 | 17.0 ± 4.7 |
| 50 | 1,2,4-Benzenetricarboxylic acid |  | 528-44-9 | 63 ± 6 | 63 ± 6 | 4.31 ± 0.72 | 22.5 ± 9.3 |
| 50 | Trimesic acid |  | 554-95-0 | 49 ± 12 | 49 ± 12 | 2.94 ± 1.10 | 34.1 ± 12.2 |
| 50 | 1,2,4,5-Benzenetetracarboxylic acid |  | 89-05-4 | 53 ± 3 | 53 ± 3 | 3.28 ± 0.25 | 42.2 ± 11.9 |
| 50 | Mellitic acid |  | 517-60-2 | 19 ± 15 | 19 ± 15 | 0.91 ± 0.80 | 27.3 ± 5.8 |
| 50 | p-Toluic acid |  | 99-94-5 | 4 ± 16 | 4 ± 16 | 0.17 ± 0.67 | 18.5 ± 3.4 |
| 50 | 4-Isopropylbenzoic acid |  | 536-66-3 | 14 ± 7 | 14 ± 7 | 0.64 ± 0.37 | 26.8 ± 6.8 |
| 50 | 4-Tert-butylbenzoic acid |  | 98-73-7 | 0 ± 19 | 0 ± 19 | 0 ± 0.87 | 25.0 ± 7.3 |
| 50 | Salicylic acid |  | 69-72-7 | 26 ± 31 | 26 ± 31 | 1.30 ± 1.87 | 23.9 ± 10.4 |
| 50 | 3-Hydroxybenzoic acid |  | 99-06-9 | -79 ± 27 | -44 ± 8 | -2.54 ± 0.63 | 23.9 ± 2.0 |
| 50 | 4-Hydroxybenzoic acid |  | 99-96-7 | -118 ± 16 | -54 ± 3 | -3.38 ± 0.33 | 16.2 ± 2.5 |
| 50 | 3,4-Dihydroxybenzoic acid |  | 99-50-3 | -131 ± 10 | -57 ± 2 | -3.63 ± 0.19 | 14.7 ± 0.9 |
| saturated | 4-Hydroxy-3,5-dimethoxybenzoic acid |  | 530-57-4 | 12 ± 12 | 12 ± 12 | 0.53 ± 0.58 | 13.7 ± 2.5 |
| 50 | 3-Methylsalicylic acid |  | 83-40-9 | 55 ± 3 | 55 ± 3 | 3.50 ± 0.27 | 38.5 ± 12.0 |
| 50 | 4-Methylsalicylic acid |  | 50-85-1 | 51 ± 18 | 51 ± 18 | 3.07 ± 1.77 | 25.4 ± 5.9 |
| 50 | 5-Methylsalicylic acid |  | 89-56-5 | 61 ± 6 | 61 ± 6 | 4.13 ± 0.71 | 27.4 ± 2.6 |
| 50 | Mandelic acid |  | 90-64-2 | 11 ± 19 | 11 ± 19 | 0.49 ± 0.95 | 25.7 ± 5.8 |
| 50 | p-Phenylenediacetic acid |  | 7325-46-4 | 6 ± 6 | 6 ± 6 | 0.28 ± 0.29 | 23.5 ± 3.8 |
| 50 | 3-Methylcinnamic acid |  | 3029-79-6 | 52 ± 15 | 52 ± 15 | 3.17 ± 1.56 | 24.2 ± 19.2 |
| 50 | 3,5-Dimethylphenylacetic acid |  | 42288-46-0 | 17 ± 14 | 17 ± 14 | 0.83 ± 0.72 | 21.1 ± 3.4 |
| 50 | 3,5-Dimethoxyphenylacetic acid |  | 4670-10-4 | 8 ± 8 | 8 ± 8 | 0.37 ± 0.36 | 10.9 ± 2.3 |
| saturated | 3,5-Dimethoxybenzyl Alcohol |  | 705-76-0 | -10 ± 21 | -9 ± 17 | -0.42 ± 0.82 | 10.6 ± 2.1 |
| 50 | 2,4-Dimethoxybenzyl alcohol |  | 7314-44-5 | -13 ± 22 | -11 ± 19 | -0.52 ± 0.92 | 13.9 ± 4.4 |
| 50 | DL-4-Hydroxy-3-methoxymandelic acid |  | 55-10-7 | 0 ± 14 | 0 ± 13 | -0.01 ± 0.61 | 19.4 ± 3.0 |
| saturated | 1-Pheny-1,3-butanedione |  | 93-91-4 | -6 ± 22 | -6 ± 21 | -0.26 ± 1.01 | 26.6 ± 9.2 |
| Saturated | Dimethyl 5-hydroxyisophthalate |  | 235-899-0 | 8 ± 20 | 8 ± 19 | 0.37 ± 0.96 | 26.5 ± 4.0 |
| saturated | 2'-Hydroxy-4'-methoxyaceto-phenone |  | 552-41-0 | 23 ± 19 | 23 ± 19 | 1.16 ± 1.19 | 21.6 ± 3.1 |
| saturated | n-Octyl gallate |  | 1034-01-1 | 33 ± 10 | 33 ± 10 | 1.76 ± 0.62 | 24.9 ± 5.4 |
| Saturated | 2,6-Bis(hydroxymethyl)-p-cresol |  | 91-04-3 | -17 ± 21 | -15 ± 14 | -0.69 ± 0.74 | 17.8 ± 2.4 |
| saturated | 2-Hydroxy-1,4-Naphtoquinone |  | 83-72-7 | 14 ± 18 | 14 ± 18 | 0.64 ± 0.86 | 32.7 ± 8.5 |
| 50 | Salicylaldehyde |  | 90-02-8 | 30 ± 8 | 30 ± 8 | 1.55 ± 0.48 | 35.5 ± 7.0 |
| 50 | Trans-cinnamaldehyde |  | 14371-10-9 | 27 ± 18 | 27 ± 18 | 1.34 ± 1.13 | 26.0 ± 6.2 |
| 50 | (R)-(−)-Glycidyl benzyl ether |  | 14618-80-5 | -72 ± 20 | -42 ± 8 | -2.36 ± 0.53 | 17.5 ± 3.1 |
| 50 | (S)-(+)-Glycidyl benzyl ether |  | 16495-13-9 | -19 ± 11 | -16 ± 8 | -0.77 ± 0.42 | 21.3 ± 0.8 |
| 50 | Tannic acid |  | 1401-55-4 | -28 ± 11 | -22 ± 7 | -1.06 ± 0.38 | 17.7 ± 3.7 |
| saturated | Maltol |  | 118-71-8 | -155 ± 4 | -61 ± 1 | -4.06 ± 0.07 | 20.4 ± 15.9 |
| 50 | Kojic acid |  | 501-30-4 | -54 ± 39 | -35 ± 17 | -1.88 ± 1.09 | 14.4 ± 1.1 |
| 50 | Furylacrylic acid |  | 539-47-9 | 4 ± 28 | 4 ± 24 | 0.17 ± 1.23 | 20.1 ± 1.9 |
| 50 | 2-Nitrobenzoic acid |  | 552-16-9 | -95 ± 27 | -49 ± 8 | -2.89 ± 0.61 | 15.0 ± 1.9 |
| 50 | 3-Methyl-2-nitrobenzoic acid |  | 5437-38-7 | -248 ± 25 | -71 ± 21 | -5.42 ± 0.31 | 6.8 ± 1.7 |
| 50 | 2-Nitroterephthalic acid |  | 610-29-7 | -17 ± 28 | -14 ± 25 | -0.68 ± 1.11 | 29.6 ± 9.2 |
| 50 | 3-Nitrophthalic acid |  | 603-11-2 | -25 ± 29 | -20 ± 20 | -0.97 ± 1.05 | 21.4 ± 3.6 |
| 50 | 4-Nitrophthalic acid |  | 610-27-5 | 17 ± 38 | 17 ± 34 | 0.81 ± 1.92 | 32.7 ± 10.4 |
| saturated | 3-Nitrosalicylic acid |  | 85-38-1 | -1 ± 18 | -1 ± 15 | -0.05 ± 0.73 | 24.1 ± 4.5 |
| 50 | 3-Hydroxy-4-nitrobenzoic acid |  | 619-14-7 | -17 ± 44 | -14 ± 33 | -0.67 ± 1.75 | 28.8 ± 8.0 |
| saturated | 3,5-Dinitrosalicylic acid |  | 609-99-4 | 16 ± 28 | 16 ± 28 | 0.75 ± 1.53 | 29.5 ± 4.1 |
| 50 | 4-Aminosalicylic acid |  | 65-49-6 | 55 ± 2 | 55 ± 2 | 3.50 ± 0.17 | 20.3 ± 5.3 |
| saturated | 5-Aminosalicylic acid |  | 89-57-6 | 63 ± 9 | 63 ± 9 | 4.35 ± 1.25 | 28.2 ± 7.6 |
| 50 | 3-Amino-4Hydroxybenzoic acid |  | 1571-72-8 | -78 ± 17 | -44 ± 5 | -2.50 ± 0.39 | 24.9 ± 2.6 |
| 50 | 2-Amino-5-methylbenzoic acid |  | 2941-78-8 | 50 ± 15 | 50 ± 15 | 3.05 ± 1.26 | 37.3 ± 10.7 |
| 50 | 2-Aminoterephthalic acid |  | 10312-55-7 | 32 ± 17 | 32 ± 17 | 1.68 ± 1.12 | 24.1 ± 9.2 |
| 50 | 5-Aminoisophthalic acid |  | 99-31-0 | 37 ± 22 | 37 ± 22 | 2.04 ± 1.55 | 24.4 ± 12.6 |
| 50 | Pyrazinecarboxylic acid |  | 98-97-5 | 5 ± 3 | 5 ± 3 | 0.23 ± 0.14 | 18.7 ± 3.4 |
| Saturated | 2,5-Pyrazinedicarboxylic acid dihydrate |  | 205692-63-3 | -26 ± 37 | -21 ± 26 | -1 ± 1.37 | 24.1 ± 5.0 |
| 50 | 2-Picolinic acid |  | 98-98-6 | 19 ± 11 | 19 ± 11 | 0.92 ± 0.59 | 14.5 ± 2.4 |
| 50 | Nicotinic acid |  | 59-67-6 | 25 ± 13 | 25 ± 13 | 1.22 ± 0.75 | 32.9 ± 4.1 |
| 50 | 3-(Pyridin-4-yl)acrylic acid |  | 5337-79-1 | -55 ± 29 | -36 ± 12 | -1.91 ± 0.81 | 17.4 ± 4.0 |
| 50 | trans-3-(3-Pyridyl)acrylic acid |  | 19337-97-4 | 21 ± 12 | 21 ± 12 | 1.03 ± 0.64 | 23.7 ± 7.4 |
| 50 | 2-Aminopyridine-3-carboxylic acid |  | 5345-47-1 | -28 ± 24 | -22 ± 13 | -1.08 ± 0.76 | 21.6 ± 8.0 |
| 50 | 2,3-Pyridinedicarboxylic acid |  | 89-00-9 | 34 ± 22 | 34 ± 22 | 1.81 ± 1.67 | 17.9 ± 6.2 |
| 50 | 2,5-Pyridinedicarboxylic acid |  | 100-26-5 | 51 ± 7 | 51 ± 7 | 3.11 ± 0.61 | 27.2 ± 3.7 |
| 50 | 2,6-Pyridinedicarboxylic acid |  | 499-83-2 | 33 ± 18 | 33 ± 18 | 1.71 ± 1.14 | 14.5 ± 3.1 |
| 50 | Dimethyl 2,6-pyridinedicarboxylate |  | 5453-67-8 | -4 ± 22 | -4 ± 20 | -0.17 ± 0.95 | 21.0 ± 3.3 |
| 50 | 3,4-Pyridinedicarboxylic acid |  | 490-11-9 | 46 ± 17 | 46 ± 17 | 2.67 ± 1.21 | 20.7 ± 10.0 |
| saturated | 2-2-Bipyridine-4-4-dicarboxylic acid |  | 6813-38-3 | 11 ± 12 | 11 ± 12 | 0.48 ± 0.58 | 35.6 ± 5.5 |
| 50 | CyDTA /trans-12-diamino |  | 125572-95-4 | -179 ± 24 | -64 ± 3 | -4.45 ± 0.38 | 4.3 ± 0.4 |
| 50 | Folic acid |  | 59-30-3 | -3 ± 20 | -3 ± 18 | -0.14 ± 0.86 | 23.0 ± 7.3 |
| saturated | α-Cyano-3-hydroxycinnamic acid |  | 28166-41-8 | -103 ± 36 | -51 ± 9 | -3.07 ± 0.77 | 24.5 ± 4.0 |
| 50 | Salicylaldoxime |  | 94-67-7 | -58 ± 27 | -37 ± 14 | -1.99 ± 0.71 | 30.0 ± 9.2 |
| 50 | Salicylhydroxamic acid |  | 89-73-6 | -54 ± 19 | -35 ± 8 | -1.87 ± 0.54 | 11.7 ± 1.8 |
| 50 | Quinaldic acid |  | 93-10-7 | -6 ± 20 | -5 ± 16 | -0.24 ± 0.80 | 35.2 ± 9.3 |
| Saturated | Chitosan |  | 9012-76-4 | 18 ± 2 | 18 ± 2 | 0.88 ± 0.11 | 23.6 ± 6.3 |
| 50 | Ethylenediamine |  | 107-15-3 | -454 ± 22 | -82 ± 1 | -7.43 ± 0.17 | 11.6 ± 1.0 |
| 50 | L-Asparagine |  | 70-47-3 | -124 ± 30 | -55 ± 6 | -3.5 ± 0.56 | 15.1 ± 0.8 |
| 50 | Ethylenediaminetetraacetic acid (EDTA) |  | 60-00-4 | -205 ± 15 | -67 ± 2 | -4.85 ± 0.22 | 3.6 ± 0.4 |
| 50 | Urea |  | 57-13-6 | 2 ± 26 | 2 ± 26 | 0.07 ± 1.06 | 23.3 ± 2.6 |
| 50 | Acetamide |  | 60-35-5 | -29 ± 25 | -22 ± 14 | -1.09 ± 0.81 | 20.5 ± 7.4 |
| 50 | N-Lauroylsarcosine Na |  | 137-16-6 | 22 ± 12 | 22 ± 12 | 1.1 ± 0.72 | 27.8 ± 7.6 |
| 50 | Glycyl-glycine |  | 556-50-3 | -164 ± 31 | -62 ± 8 | -4.21 ± 0.51 | 17.0 ± 2.9 |
| 50 | L-Ornithine hydrochloride |  | 3184-13-2 | -266 ± 40 | -73 ± 4 | -5.64 ± 0.50 | 13.9 ± 1.4 |
| 50 | Aspartic acid |  | 56-84-8 | -76 ± 7 | -43 ± 2 | -2.46 ± 0.18 | 14.0 ± 1.7 |
| 50 | 5,5-Dimethylhydantoin |  | 77-71-4 | -312 ± 22 | -76 ± 1 | -6.15 ± 0.22 | 18.7 ± 1.2 |
| 50 | Diethylenetriaminepentaacetic acid |  | 67-43-6 | -270 ± 15 | -73 ± 1 | -5.68 ± 0.17 | 4.7 ± 0.2 |
| 50 | L-Cysteine |  | 52-90-4 | -84 ± 14 | -46 ± 4 | -2.64 ± 0.32 | 13.9 ± 1.5 |
| 50 | N-(2-Trisodium (2-hydroxyethyl)ethylenediaminetriacetate |  | 139-89-9 | -155 ± 7 | -61 ± 1 | -4.06 ± 0.11 | 5.6 ± 1.0 |
| 50 | 2,2′-(Ethylenedioxy)bis(ethylamine) |  | 929-59-9 | -200 ± 11 | -67 ± 1 | -4.77 ± 0.15 | 12.9 ± 2.2 |
| 50 | Glycine |  | 56-40-6 | -155 ± 30 | -61 ± 4 | -4.07 ± 0.49 | 18.1 ± 2.9 |
| 50 | Lysine |  | 56-87-1 | -139 ± 34 | -58 ± 6 | -3.79 ± 0.61 | 14.4 ± 3.2 |
| 50 | Iminodiacetic acid |  | 142-73-4 | -149 ± 22 | -60 ± 4 | -3.95 ± 0.39 | 5.8 ± 3.0 |
| 50 | N-(2-Hydroxyethyl)iminodiacetic acid |  | 93-62-9 | -161 ± 48 | -62 ± 7 | -4.17 ± 0.81 | 11.7 ± 0.7 |
| 50 | 2-Amino-2-methyl-1,3-propanediol |  | 115-69-5 | -271 ± 22 | -73 ± 2 | -5.70 ± 0.26 | 14.8 ± 2.7 |
| 50 | BIS-TRIS |  | 6976-37-0 | -126 ± 16 | -56 ± 3 | -3.54 ± 0.3 | 19.2 ± 2.4 |
| 50 | BIS-TRIS propane |  | 64431-96-5 | -190 ± 31 | -66 ± 4 | -4.63 ± 0.46 | 14.5 ± 2.6 |
| 50 | Hexamethyleneteramine |  | 100-97-0 | -52 ± 35 | -34 ± 14 | -1.82 ± 0.94 | 20.3 ± 4.8 |
| 50 | Piperazine |  | 110-85-0 | -34 ± 10 | -25 ± 5 | -1.27 ± 0.31 | 17.4 ± 3.5 |
| 50 | Pyrazine |  | 290-37-9 | -37 ± 24 | -27 ± 13 | -1.36 ± 0.75 | 10.6 ± 3.0 |
| saturated | Uracil |  | 66-22-8 | -113 ± 55 | -53 ± 16 | -3.29 ± 1.26 | 20.6 ± 7.3 |
| 50 | 1-(2-Hydroxyethyl)piperazine |  | 103-76-4 | -134 ± 13 | -57 ± 2 | -3.70 ± 0.25 | 13.7 ± 3.1 |
| saturated | 1,10-Phenanthroline monohydrate |  | 66-71-7 | 19 ± 16 | 19 ± 16 | 0.94 ± 0.94 | 28.4 ± 3.7 |
| saturated | 2,2'-Bipyridyl |  | 366-18-7 | 27 ± 12 | 27 ± 12 | 1.35 ± 0.65 | 20.1 ± 3.8 |
| saturated | 5-Nitrobarbituric acid trihydrate |  | 209529-81-7 | 42 ± 18 | 42 ± 18 | 2.38 ± 1.25 | 36.0 ± 3.9 |
| 50 | Pyrazole |  | 288-13-1 | 20 ± 9 | 20 ± 9 | 0.99 ± 0.51 | 20.8 ± 2.5 |
| 50 | Benzotriazole |  | 95-14-7 | -107 ± 16 | -52 ± 4 | -3.17 ± 0.35 | 30.0 ± 7.0 |
| 50 | 1,2,4-Triazole |  | 288-88-0 | -283 ± 21 | -74 ± 1 | -5.83 ± 0.24 | 17.9 ± 5.4 |
| 50 | 3,5-Dimethylpyrazole |  | 67-51-6 | -24 ± 30 | -19 ± 20 | -0.93 ± 1.05 | 19.1 ± 5.9 |
| 50 | 3-Hydroxy-1,2-dimethyl-4(1H)-pyridone |  | 30652-11-0 | -138 ± 15 | -58 ± 3 | -3.76 ± 0.27 | 6.0 ± 1.2 |
| Saturated | 5-Nitro-1,10-phenanthroline |  | 4199-88-6 | -6 ± 39 | -6 ± 30 | -0.26 ± 1.61 | 20.1 ± 4.4 |
| 50 | 3,5-Dimethylpyrazole-1-methanol |  | 85264-33-1 | 28 ± 19 | 28 ± 19 | 1.41 ± 1.26 | 24.1 ± 5.2 |
| Saturated | 5-Nitrouracil |  | 611-08-5 | 35 ± 11 | 35 ± 11 | 1.87 ± 0.77 | 25.7 ± 4.3 |
| 50 | N,N′-Trimethyleneurea |  | 1852-17-1 | 8 ± 10 | 8 ± 10 | 0.38 ± 0.45 | 20.1 ± 2.5 |
| 50 | Benzamide |  | 55-21-0 | 17 ± 19 | 17 ± 19 | 0.78 ± 0.99 | 24.6 ± 8.9 |
| 50 | 4-Amino-4H-1,2,4-triazole |  | 584-13-4 | -22 ± 11 | -18 ± 8 | -0.87 ± 0.40 | 20.4 ± 2.4 |
| saturated | 8-Hydroxyquinoline |  | 148-24-3 | -14 ± 12 | -12 ± 9 | -0.55 ± 0.46 | 14.7 ± 3.7 |
| 50 | 6-Hydroxyquinoline |  | 580-16-5 | -23 ± 13 | -19 ± 8 | -0.92 ± 0.45 | 23.2 ± 5.1 |
| 50 | 8-Aminoquinoline |  | 578-66-5 | -76 ± 21 | -43 ± 6 | -2.45 ± 0.48 | 18.7 ± 6.2 |
| saturated | 5-Aminoisoquinoline |  | 1125-60-6 | 62 ± 5 | 62 ± 5 | 4.26 ± 0.59 | 22.6 ± 5.3 |
| 50 | 8-Nitroquinoline |  | 607-35-2 | -3 ± 26 | -3 ± 23 | -0.15 ± 1.13 | 23.1 ± 2.5 |
| 50 | 4-Quinolinol |  | 611-36-9 | -23 ± 16 | -18 ± 11 | -0.89 ± 0.57 | 23.3 ± 3.5 |
| saturated | 6-Aminoindole |  | 5318-27-4 | 34 ± 7 | 34 ± 7 | 1.79 ± 0.48 | 18.8 ± 0.7 |
| saturated | 5-Aminoindole |  | 5192-03-0 | 18 ± 7 | 18 ± 7 | 0.85 ± 0.39 | 16.6 ± 2.5 |
| 50 | 1-Octanethiol |  | 111-88-6 | 11 ± 5 | 11 ± 5 | 0.50 ± 0.26 | 19.6 ± 6.8 |
| 50 | 1-Dodecanethiol |  | 112-55-0 | 0 ± 24 | 0 ± 20 | 0.01 ± 0.97 | 20.7 ± 6.5 |
| SA50 | 1-Undecanethiol |  | 5332-52-5 | -31 ± 23 | -24 ± 14 | -1.18 ± 0.77 | 25.4 ± 3.2 |
| 50 | 2,2′-Thiodiacetic acid |  | 123-93-3 | 11 ± 13 | 11 ± 13 | 0.51 ± 0.71 | 22.2 ± 9.0 |
| /50 | 2,2′-(Ethylenedithio)diacetic acid |  | 7244-02-2 | 11 ± 5 | 11 ± 5 | 0.49 ± 0.26 | 24.0 ± 12.3 |
| 50 | 4,4′-Dithiodibutyric acid |  | 2906-60-7 | 7 ± 22 | 7 ± 22 | 0.31 ± 1.18 | 31.4 ± 11.0 |
| 50 | Thiourea |  | 62-56-6 | 72 ± 4 | 72 ± 4 | 5.60 ± 0.63 | 25.3 ± 9.8 |
| 50 | Sodium-2mercaptoethanesulfonate |  | 19767-45-4 | -140 ± 26 | -58 ± 5 | -3.80 ± 0.47 | 19.1 ± 15.6 |
| 50 | Taurine |  | 107-35-7 | -38 ± 26 | -28 ± 12 | -1.40 ± 0.77 | 8.9 ± 9.6 |
| 50 | N-(2-acetamido)-2-aminoethanesulfonic acid (ACES) |  | 7365-82-4 | -173 ± 29 | -63 ± 4 | -4.36 ± 0.44 | 17.7 ± 3.0 |
| 50 | Sodium diethyldithiocarbamate |  | 20624-25-3 | 26 ± 9 | 26 ± 9 | 1.34 ± 0.54 | 22.5 ± 4.3 |
| 50 | TAPSO |  | 68399-81-5 | -176 ± 27 | -64 ± 4 | -4.40 ± 0.44 | 22.0 ± 1.6 |
| 50 | Methionine |  | 63-68-3 | -106 ± 37 | -52 ± 9 | -3.15 ± 0.79 | 18.9 ± 5.7 |
| 50 | AMPSO |  | 68399-79-1 | -150 ± 13 | -60 ± 2 | -3.98 ± 0.23 | 18.0 ± 3.8 |
| 50 | TAPS |  | 29915-38-6 | -92 ± 30 | -48 ± 8 | -2.83 ± 0.65 | 22.6 ± 4.5 |
| 50 | EPPS |  | 16052-06-5 | -154 ± 22 | -61 ± 3 | -4.05 ± 0.37 | 18.4 ± 2.6 |
| 50 | 2-Mercaptopyridine-3-carboxylic acid |  | 38521-46-9 | -21 ± 31 | -17 ± 18 | -0.83 ± 1.03 | 29.3 ± 17.4 |
| 50 | 6-Mercaptopyridine-3-carboxylic acid |  | 92823-43-3 | -88 ± 37 | -47 ± 10 | -2.74 ± 0.82 | 8.6 ± 2.7 |
| saturated | Sodium dodecylbenzene sulfonate |  | 25155-30-0 | 77 ± 6 | 77 ± 6 | 6.43 ± 1.24 | 37.0 ± 9.3 |
| 50 | Penicillin G Na salt |  | 69-57-8 | -39 ± 25 | -28 ± 13 | -1.44 ± 0.78 | 40.4 ± 2.4 |
| Saturated | Anthraquinone-2-sulfonic acid sodium salt monohydrate |  | 153277-35-1 | -41 ± 10 | -29 ± 5 | -1.5 ± 0.32 | 10.5 ± 0.8 |
| 50 | 5-Sulfosalicylic acid |  | 5965-83-3 | -79 ± 6 | -44 ± 2 | -2.52 ± 0.14 | 12.3 ± 3.2 |
| 1 | Hydroquinonesulfonic acid potassium salt |  | 21799-87-1 | -18 ± 41 | -15 ± 32 | -0.72 ± 1.54 | 8.9 ± 4.3 |
| 50 | 8-Anilino-1-naphthalenesulfonic acid ammonium salt |  | 28836-03-5 | 12 ± 12 | 12 ± 12 | 0.53 ± 0.58 | 41.7 ± 11.9 |
| saturated | 8-Hydroxy-5-quinoline sulfonic acid |  | 207386-92-3 | -119 ± 26 | -54 ± 6 | -3.4 ± 0.52 | 9.4 ± 0.9 |
| saturated | 8-Hydroxy-7-iodo-5-quinolinesulfonic acid |  | 547-91-1 | -56 ± 28 | -36 ± 12 | -1.94 ± 0.80 | 17.2 ± 7.9 |
| 50 | 2-(Cyclohexylamino)ethanesulfonic acid (CHES) |  | 103-47-9 | -181 ± 30 | -64 ± 4 | 4.48 ± 0.48 | 18.1 ± 4.0 |
| 50 | 3-Mercaptobenzoic acid |  | 4869-59-4 | 46 ± 25 | 46 ± 25 | 2.69 ± 1.83 | 33.0 ± 10.3 |
| 50 | 4-Mercaptobenzoic acid |  | 1074-36-8 | 32 ± 18 | 32 ± 18 | 1.67 ± 1.17 | 44.8 ± 8.9 |
| 50 | 2-Mercaptobenzoic acid |  | 147-93-3 | -7 ± 18 | -7 ± 14 | -0.29 ± 0.68 | 17.3 ± 7.4 |
| 50 | 2,5-Thiophenedicarboxylic acid |  | 4282-31-9 | 74 ± 10 | 74 ± 10 | 5.89 ± 1.98 | 32.3 ± 6.6 |
| 50 | 3-(2-Thienyl)acrylic acid |  | 15690-25-2 | -8 ± 3 | -7 ± 2 | -0.30 ± 1.12 | 16.4 ± 3.8 |
| 50 | 1,3,4-thiadiazole-2,5-dithiol (DMTD, bismuthiol) salt |  | 1072-71-5 | 87 ± 6 | 87 ± 6 | 9.02 ± 2.03 | 5.4 ± 0.9 |
| 50 | 5-Amino-1,3,4-thiadiazole-2-thiol |  | 2349-67-9 | 59 ± 8 | 59 ± 8 | 3.90 ± 0.87 | 56.0 ± 4.3 |
| Saturated | 2-Amino-5-trifluoromethyl-1,3,4-thiadiazole |  | 10444-89-0 | 48 ± 6 | 48 ± 6 | 2.83 ± 0.52 | 29.2 ± 7.2 |
| 50 | 2,5-Dimethyl-1,3,4-thiadiazole |  | 27464-82-0 | -1 ± 12 | -1 ± 12 | -0.05 ± 0.55 | 21.4 ± 1.9 |
| Saturated | 4-Amino-6-mercaptopyrazolo[3,4-d]pyrimidine |  | 23771-52-0 | 40 ± 13 | 40 ± 13 | 2.20 ± 0.97 | 28.1 ± 4.2 |
| 50 | 4,5-Diamino-2,6-dimercaptopyrimidine |  | 31295-41-7 | 36 ± 21 | 36 ± 21 | 1.96 ± 1.56 | 29.2 ± 4.8 |
| Saturated | 4-Amino-3-hydrazino-5-mercapto-1,2,4-triazole |  | 1750-12-5 | 32 ± 10 | 32 ± 10 | 1.66 ± 0.63 | 26.8 ± 3.8 |
| Saturated | 4,6-Diamino-2-pyrimidinethiol |  | 1004-39-3 | 28 ± 9 | 28 ± 9 | 1.44 ± 0.49 | 31.1 ± 3.2 |
| 50 | 2,6-Diamino-4-chloropyrimidine |  | 156-83-2 | 1 ± 21 | 1 ± 20 | 0.04 ± 0.99 | 28.1 ± 4.7 |
| Saturated | 2-Mercapto-5-methylbenzimidazole |  | 27231-36-3 | 43 ± 7 | 43 ± 7 | 2.48 ± 0.49 | 34.6 ± 6.4 |
| 50 | 2-Mercapto-1-methylimidazole |  | 60-56-0 | -35 ± 15 | -26 ± 9 | -1.32 ± 0.50 | 25.4 ± 9.1 |
| 50 | 2-Mercaptoimidazole |  | 872-35-5 | -5 ± 17 | -5 ± 16 | -0.2 ± 0.75 | 30.5 ± 6.3 |
| 50 | Sodium phosphite |  | 13517-23-2 | 45 ± 3 | 45 ± 3 | 2.63 ± 0.24 | 10.9 ± 1.9 |
| Saturated | (12-Phosphonododecyl)phosphonic acid |  | 7450-59-1 | 20 ± 16 | 20 ± 16 | 0.98 ± 0.96 | 24.9 ± 8.0 |
| 50 | Ethylphosphonic acid |  | 6779-09-5 | -73 ± 13 | -42 ± 5 | -2.37 ± 0.34 | 18.3 ± 0.4 |
| 50 | Propylphosphonic acid |  | 4672-38-2 | -75 ± 34 | -43 ± 11 | -2.42 ± 0.84 | 22.0 ± 4.5 |
| 50 | Hexylphosphonic acid |  | 4721-24-8 | 18 ± 11 | 18 ± 11 | 0.87 ± 0.57 | 32.4 ± 4.5 |
| 50 | Butylphosphonic acid |  | 3321-64-0 | -32 ± 42 | -24 ± 23 | -1.19 ± 1.33 | 25.4 ± 6.9 |
| Saturated | Octylphosphonic acid |  | 4724-48-5 | 45 ± 20 | 45 ± 20 | 2.58 ± 1.38 | 23.9 ± 3.8 |
| 50 | Decylphosphonic acid |  | 6874-60-8 | 11 ± 23 | 1 ± 22 | 0.52 ± 1.23 | 19.9 ± 5.4 |
| 50 | n-Dodecylphosphonic acid |  | 5137-70-2 | -11 ± 20 | -10 ± 16 | -0.47 ± 0.77 | 20.6 ± 2.8 |
| 50 | Tetradecylphosphonic acid |  | 4671-75-4 | -34 ± 17 | -25 ± 11 | -1.26 ± 0.58 | 18.1 ± 4.9 |
| Saturated | Hexadecylphosphonic acid |  | 4721-17-9 | -45 ± 6 | -31 ± 3 | -1.6 ± 0.19 | 21.1 ± 6.0 |
| Saturated | Octadecylphosphonic acid |  | 4724-47-4 | -30 ± 29 | -23 ± 19 | -1.14 ± 0.99 | 22.3 ± 1.7 |
| 50 | Diethyl cyanomethylphosphonate |  | 2537-48-6 | -226 ± 43 | -69 ± 4 | -5.14 ± 0.55 | 13.0 ± 1.3 |
| 50 | Diethyl (2-methylallyl) phosphonate |  | 51533-70-1 | 5 ± 13 | 5 ± 1 | 0.22 ± 0.57 | 24.1 ± 3.8 |
| 50 | Methylphosphonic acid |  | 993-13-5 | -29 ± 33 | -22 ± 24 | -1.1 ± 1.25 | 14.7 ± 3.7 |
| 50 | Diethyl allylphosphonate |  | 1067-87-4 | -17 ± 10 | -14 ± 8 | -0.67 ± 0.40 | 11.3 ± 6.2 |
| 50 | Etidronic acid |  | 2809-21-4 | -94 ± 9 | -49 ± 2 | -2.88 ± 0.20 | 4.3 ± 0.1 |
| 50 | 6-Phosphonohexanoic acid |  | 5662-75-9 | -38 ± 11 | -28 ± 6 | -1.4 ± 0.33 | 21.5 ± 5.3 |
| 50 | Hypophosphorous acid |  | 6303-21-5 | -64 ± 11 | -39 ± 4 | -2.16 ± 0.29 | 14.9 ± 3.7 |
| 50 | Phytic acid |  | 83-86-3 | -108 ± 15 | -52 ± 4 | -3.18 ± 0.32 | 18.2 ± 6.8 |
| 50 | (3-Bromopropyl) phosphonic acid |  | 1190-09-6 | -115 ± 22 | -53 ± 5 | -3.32 ± 0.46 | 22.3 ± 2.6 |
| 50 | Diethyl (bromodifluoromethyl) phosphonate |  | 65094-22-6 | -132 ± 12 | -57 ± 2 | -3.66 ± 0.23 | 22.1 ± 4.2 |
| 50 | Nitrilotri(methylphosphonic acid) |  | 6419-19-8 | -108 ± 48 | -52 ± 14 | -3.18 ± 1.12 | 13.3 ± 4.8 |
| 50 | Glyphosine |  | 2439-99-8 | -69 ± 33 | -41 ± 14 | -2.27 ± 0.94 | 10.0 ± 1.0 |
| 50 | Phenylphosphonic acid |  | 1571-33-1 | -1 ± 15 | -1 ± 13 | -0.06 ± 0.63 | 23.7 ± 3.4 |
| 50 | Heptyltriphenylphosphonium bromide |  | 13423-48-8 | -29 ± 33 | -22 ± 21 | -1.1 ± 1.13 | 18.66 ± 5.3 |